| COOMET PROJECT FINAL REPORT |
| --- |
| 1. Ref No.: 457/RU-a/09 | 2. Subject field: Certified REFERENCE MATERIALS |
| 3. Field of cooperation: RESEARCH |
| 4. Working Group: Belarus, Kyrgyzstan, Russia, Ukraine, Uzbekistan |
| 5. Subject: Development of CRM for composition of belov cenosphere concentrate (CBC-1) |
| 6. Progress: The development of CRM for composition of magnetic cenosphere concentrate (CMC-2)* is completed. The organizations of Belarus, Kyrgyzstan, Mongolia, Russia, Ukraine and Uzbekistan took part in certification analyses. The developed CRM is approved in Russia as state CRM under the number CRM 9235-2008. The report on CRM development and documentation on CRM were preliminary circulated among the national bodies of COOMET member-countries of the Contact Persons of TC 1.12 “CRMs”, agreed at the 14th COOMET meeting of COOMET TC 1.12 “CRMs”. The decision was taken to include CRM for composition of magnetic cenosphere concentrate (CMC-2) in the List of CRMs, agreed for the recognition as COOMET CRMs to be submitted to the 20th COOMET Committee meeting (April, 2010). CRM for composition of magnetic cenosphere concentrate (CMC-2) was recognized as COOMET CRM at the 20th COOMET Committee meeting (resolution 25 of the minutes) and registered in the Register of COOMET CRMs under the number COOMET CRM 0095-2010-RU. ARMENIA, BELARUS, BULGARIA, KAZAKHSTAN, KYRGYZSATAN, LITHUANIA, MOLDOVA and UKRAINE joined the CRM recognition as COOMET CRM. CRM is intended for error control of measurement procedures, used in the determination of chemical composition of coal fly ash, slag and extracted fractions. CRM can be used for verification (calibration) and graduation of measurement instruments, provided that their metrological characteristics meet specified criteria. The areas of application are heat power industry, building industry, coal industry, geology, environment protection, chemical industry, scientific research. * During CRM development it was found reasonable to substitute the name “CRM for composition of belov cenosphere concentrate (CBC-1)” for “CRM for composition of magnetic cenosphere concentrate (CMC-2)” to avoid reference to the place of coal combustion, since the concentrate composition does not depend on the type of the boiler, used in energy company. Accordingly the index of CRM of belov cenosphere concentrate “CBC-1” was substituted for “CMC-2”. |
| 7. Coordinator’s name: Irina E.Vasilyeva, Head of laboratory of A.P. Vinogradov Geochemistry Institute, Siberian Branch of RAS Address: 1a, Favorsky Str., Irkutsk, 664033 Telephone: (3952) 42 58 37 Fax: (3952) 42 70 50 E-mail: vasira@igc.irk.ru |
| 8. Completion date: May, 2010 |
| 9. Coordinator’s signature: | 10. Date: 25.05.2010 |