| COOMET PROJECT FINAL REPORT |
| --- |
| 1 Ref. №: 249/KZ/01 | 2 Subject field: Certified reference materials |
| 3 Field of cooperation: Development and use of certified reference materials for composition and properties of substances and materials |
| 4 Working Group: Kazakhstan, Kyrgyzstan, Russia |
| 5 Subject: Development of CRM for composition of gas conduit dust in the production of lead and zinc. |
| 6 Progress: Certified Reference Material for composition of gas conduit dust in the production of lead and zinc is developed. CRM metrological characteristics are obtained by interlaboratory certification, performed in laboratories of Kazakhstan, Russia, Kyrgyzstan and Uzbekistan and are in conformity with characteristics claimed in the project 249/KZ/01. Certificate of Type Approval No. 240 for CRM for composition of gas conduit dust in the production of lead and zinc, issued by Committee of technical regulation and metrology of Republic of Kazakhstan is obtained (registration number in the Register of GSI RK KZ. 03.01.00076-2008). The documents on CRM are circulated among the Contact Persons from COOMET member-countries in TC 1.12 “CRMs” for consideration. CRM for composition of gas conduit dust in the production of lead and zinc is recognized as COOMET CRM at the 13th meeting of TC 1.12 “CRMs” (May 2008, St. Petersburg, Russia) and registered in the COOMET Register of CRMs under number 0062-2008-KZ. Armenia, Belarus, Bulgaria, Georgia, Kyrgyzstan, Russia, Slovakia, Ukraine joined to the recognition of the CRM as COOMET CRM. |
| 7 Coordinator’s name: L.N. Yamshikova (Head of standardization and metrology laboratory, DGP “VNIITSVETMET”) Address: 1, Promyshlennaya Str., Ust-Kamenogorsk, 070002, Republic of Kazakhstan Telephone: (7232) 47-37-73 Fax: (7232) 47-37-71, 50-31-34 E-mail: vcmnauka@mail.east.telecom.kz |
| 8 Completion date: May 2008 |
| 9 Coordinator’s signature: | 10 Date: August 2008 |